## Slide 1
High throughput screening of binary intermetallics for the
direct conversion of syngas to multi-carbon oxygenates
Brook Wander, Zachary Ulissi
Carnegie Mellon University
Motivation
Synthesis gas chemistries are a pillar of the petrochemical industry. Syngas can be made from biomass. Carbon monoxide can be made from CO2 reduction reaction. With access to sustainable hydrogen, syngas chemistries could prove to be an attractive way to access value-added carbon products sustainably in a post-fossil fuel era.
Results
Conclusions
Background
Binary Intermetallic Design Space
Syngas chemistries could prove to be effective for accessing value-added multi-carbon products in a post-fossil fuel era
ML models are well suited for broad design space exploration for the discovery of novel catalysts
Contact
Brook Wander: bwander@andrew.cmu.edu
Zachary Ulissi: zulissi@andrew.cmu.edu
Background
Methods
ML Mean Absolute Errors
Deploy an interactive web dashboard of results to facilitate communication and collaboration
Consider other materials databases for broader exploration
Next Steps
Fengwang Li Group https://fengwangli.com/research
Transition Metal Candidates
Reaction network
Two descriptor microkinetic models
J.Schumann et al. ACS Catal. 2018, 8, 3447−3453
J.Schumann et al. ACS Catal. 2018, 8, 3447−3453
Chemical
Engineering
Surfaces with minimum binding energies that capture a design space with selectivity ≥ 0.1 are considered
A majority of candidates are palladium containing, which is relatively unexplored
More CuCo candidates should be considered for pipeline validation
Many elementary step networks can be reduced to functions of just 2 descriptors by developing relations between all the energies in the network and the descriptors.
Chanussot, L. et al. ACS Catal. 2021, 11, 10, 6059-6072
We consider all transition metal binary intermetallic materials. A variety of unique sites on surfaces with miller indices less than 2 are considered. This requires the calculation of 3.2 million descriptor energies.
Models were trained using the OC20 dataset, a dataset of 460,000 density functional theory calculations. The materials of interest here are well represented by the dataset.
Machine Learning (ML) Inference
Two approaches can be used. The direct approach was used to screen all 1.6 million *OH energies. The relaxation approach was used for *CO energies where the minimum *OH values over a surface were in the range considered in the microkinetic model.
Reaction Network Difficulty
Material Pipeline
Good catalysts must dissociate *CO to form *CHx intermediates, but also maintain *CO for insertion. Rhodium and CuCo systems demonstrated promise experimentally.
Rhodium
Copper - Cobalt
ML inference was parallelized using a custom dask (an open-source parallel computing platform) workflow. This allowed many calculations to be performed at one time over many cores.
Objective
Discover novel catalysts that facilitate the selective conversion of syngas to multi-carbon oxygenates.